## Slide 1: Application of additive manufacturing technology for the production of injection molding tools in order to reduce the cycle time
Zoltán Takács, Imre Kállai
8th INTERNATIONAL SCIENTIFIC CONFERENCE ON ADVANCES IN MECHANICAL ENGINEERING
(ISCAME 2022)
10-11 November, 2022 Debrecen, Hungary
GINOP-2.1.2-8-1-4-16-2017-00430

## Slide 2
What is additive manufacturing?
Additive manufacturing – defined by ASTM International (ASTM 2792 12):
Additive manufacturing is a process of joining materials to make objects from three dimensional data, usualy layer upon layer, as opposed to substractive manufacturing methodologies.
GINOP-2.1.2-8-1-4-16-2017-00430

## Slide 3
additive manufacturing vs Traditional Manufacturing
GINOP-2.1.2-8-1-4-16-2017-00430

## Slide 4
additive manufacturing technologies
GINOP-2.1.2-8-1-4-16-2017-00430

## Slide 5
Benefits of additive Manufacturing
GINOP-2.1.2-8-1-4-16-2017-00430

## Slide 6
Benefits of additive Manufacturing – how can we use it?
GINOP-2.1.2-8-1-4-16-2017-00430

## Slide 7
Injection molding cycle
GINOP-2.1.2-8-1-4-16-2017-00430

## Slide 8
Injection molding – process cycle
GINOP-2.1.2-8-1-4-16-2017-00430
Rapid Heat/Cool Technology
CONFORMAL COOLING TOOL

## Slide 9
The test products
GINOP-2.1.2-8-1-4-16-2017-00430
Main goal
Complex surface design

## Slide 10
Tool and Cooling chanel desig
GINOP-2.1.2-8-1-4-16-2017-00430

## Slide 11
Normal and conformal Cooling chanel desig
GINOP-2.1.2-8-1-4-16-2017-00430

## Slide 12
tool insert produced with additive manufacturing technology
GINOP-2.1.2-8-1-4-16-2017-00430
AFTER 3D PRINTING  SURFACE MACHINING  COMPLETE TOOL

## Slide 13
injection molding manufacturing test
GINOP-2.1.2-8-1-4-16-2017-00430
Material:
PP
PA 6
PA 6 30 GF
Cooling chanel type | Cooling chanel diameter, mm
Conventional V1 | 6
Additiv - Conformal V1 | 6
Conventional V4 | 8
Additiv - Conformal V4 | 8
Conventional V7 | 12
Additiv - Conformal V7 | 12
CONVENTIONAL TOOL
CONFORMAL TOOL

## Slide 14
injection molding test RESULTS
GINOP-2.1.2-8-1-4-16-2017-00430
+ Cooling time was reduced from 20 sec to 7 sec (-65%)
+ 3D printed tool was 15% lighter compare to the conventional one
- Tensile Strength was decreasing with 5,6%

## Slide 15
Interesting pictures
GINOP-2.1.2-8-1-4-16-2017-00430

## Slide 16
GINOP-2.1.2-8-1-4-16-2017-00430

## Slide 17
Thank you
for
your
Attention!
GINOP-2.1.2-8-1-4-16-2017-00430